CEE*QUEST 70 E

Cee*Quest 70 is a mixture of carbohydrate monomers and polymers that have been converted to chelates.  The product is intended for use as a metal ion chelating agent.  The product will chelate metals such as calcium, magnesium, iron, aluminum, manganese, zinc and copper.

PRODUCT DATA

Calcium Chelation			380 mg calcium carbonate per gram

pH 12.5 or greater

Iron Chelation			450 mg Fe3+ per gram

pH 12.5 or greater

Color					Red Brown

Odor					Ammoniacal

Specific Gravity			1.320 – 1.330 at 72oF

Density				10.99 – 11.08 lbs/gal

Solids					60.0 % (ASTM-C494)

pH					8.0 – 10.5

Crystallization Point			Below 15oF

Solubility				Miscible with water

Containers				Drums, Tank Trucks, Rail Cars

Typical Applications and Uses

Alkaline metal cleaning, derusting, descaling, and bottle washing.  Metal sequestering applications in textile or cotton processing.  Formulation of water reducing retarding mixtures for the concrete industry.

2/00