CEE*QUEST

PHOSPHORIC ACID

75% H3PO4

|  | COMPONENT | TYPICAL ANALYSIS |
| --- | --- | --- |
| CHEMICAL | Phosphoric Acid, H3PO4 | 75 % |
| SPECIFICATIONS | Solids | less than 0.2 % |
|  | Free Water | 18.0 % |
|  | Aluminum, Al2O3 | 0.61 % |
|  | Iron, Fe2O3 | 0.76 % |
|  | Magnesium, MgO | 0.23 % |
|  | Sulfate, SO4 | 2.2 % |
|  | Potassium | 0.15% |
|  | Fluoride | 0.15 % |
|  | Calcium, CaO | 10 ppm |
| PHYSICAL |  |  |
| SPECIFICATIONS | Specific Gravity 75oF | 1.67 |
|  | Weight Per Gallon | 13.9 pounds |

5/96